In polycrystalline materials, the process of grain growth monotonically decreases the free energy stored in internal interfaces [ref]. Based on this fact, prevailing theories for two-dimensional [Smith2015, Mullins1956] and three-dimensional [MacPherson2007] grain growth predict the time evolution of grain size exactly and deterministically on a grain-by-grain basis. However, while computer simulations of grain growth based on these theories accurately reproduce the statistical features of grain growth, such as grain size distribution and the time evolution of average grain size, they consistently fail to predict individual grain geometry and topology observed in experiments [McKenna2014, Peng2022]. This discrepancy is attributed to many factors, including anisotropy in grain boundary energy and/or mobility, the presence of solute species, the existence and nature of defects, and so on. Nonetheless, even as simulation methods improve to address each of these factors, disparities remain. This leads us to ask: What are the intrinsic limits on predictivity for microstructural evolution simulations?

The atomic mechanism of grain growth involves atoms near a grain boundary switching their grain memberships. Because this is intrinsically a short-range process, grain growth is expected to depend only on a grain’s local neighborhood. Indeed, grain growth theories represent that neighborhood via the grain topology (number of neighbors) [Smith2015, Mullins1956] or geometry (mean width and edge length) [Macpherson2007], both of which are local characteristics. As reflected in these theories, atom switching among neighboring grains continuously and predictably evolves the neighborhood toward a lower free energy configuration.

However, a polycrystalline microstructure is a network of connected grains. The outcomes of events that take place within this network can be transmitted over long distances and can directly and discontinuously alter a grain’s neighborhood. The classical example is a topological transformation, either a grain disappearance or a facet appearance or disappearance event [RHINES1974, DEHOFF2020]. A topological transformation discontinuously and irreversibly changes the topology (number of neighbors) and geometry (edge length) of grains in its immediate area. The resulting abrupt change in a grain’s growth rate can affect all the grains with which it interacts, and they in turn can transmit the change further afield. The effects can ultimately percolate to grains many neighbor shells removed from the original transformation.

Furthermore, topological transformations have a stochastic nature that contributes intrinsic uncertainty to microstructural evolution processes. The implications of this uncertainty on the overall grain growth process is not immediately clear. However, computational simulations suggest that it may be substantial. For example, in kinetic Monte Carlo grain growth simulations starting from identical initial conditions, Cohn showed that a given grain my grow continuously or shrink and disappear entirely due to slight differences in the timing of remote topological events [Cohn2024]. That is, small local changes may cause large and persistent global changes, e.g. a nonlinear response. It is well-known that in nonlinear systems uncertainty increases with time, and long-term predictivity is difficult or impossible [ref].

Of course, kinetic Monte Carlo simulation includes stochastic events (spin flips) at a length scale comparable to microstructural features, so results may not be representative of physical systems. Ideally, we would probe initial-condition dependence by comparing identical experimental samples, but it is impossible to create systems that are identical at the atomic scale. So instead we turn to atomistic simulations using the classical molecular dynamics (MD) method. Here we can build polycrystalline systems that are guaranteed to be identical at the scale of atomic positions, and we can evolve them to observe how uncertainty at the atomic scale propagates to affect the microstructure as a whole. We find that the effects of small-scale differences amplify over time, so that nanoscale events ultimately result in micron-scale differences in grain structure. Our conclusion is that while the statistical characteristics of a grain ensemble are predictable, individual grain growth trajectories are not. Instead, the intrinsic uncertainty increases with time throughout the evolution process.

Smith2015. Smith, C.S. Grain Shapes and Other Metallurgical Applications of Topology. Metallogr. Microstruct. Anal. 4, 543–567 (2015). https://doi.org/10.1007/s13632-015-0241-1

Mullins1956. W. W. Mullins; Two‐Dimensional Motion of Idealized Grain Boundaries. J. Appl. Phys. 1 August 1956; 27 (8): 900–904. https://doi.org/10.1063/1.1722511

MacPherson2007: MacPherson, R., Srolovitz, D. The von Neumann relation generalized to coarsening of three-dimensional microstructures. Nature 446, 1053–1055 (2007). https://doi.org/10.1038/nature05745

McKenna2014. I. M. McKenna et al. Acta Mater 78 (2014) 125

Peng2022. X. Peng et al, Phys Rev Mater 6 (2022) 033402.

RHINES1974. Rhines, F.N., Craig, K.R. & DeHoff, R.T. Mechanism of steady-state grain growth in aluminum. Metall Trans 5, 413–425 (1974). https://doi.org/10.1007/BF02644109

DEHOFF2020. Robert T. DeHoff, Burton R Patterson, Topological event rates and the evolution of the grain face distribution in grain growth, Acta Materialia, Volume 201, 2020, Pages 403-411, ISSN 1359-6454, https://doi.org/10.1016/j.actamat.2020.09.086.

Cohn2024. Cohn, R., Holm, E.A. Graph convolutional network for predicting abnormal grain growth in Monte Carlo simulations of microstructural evolution. Sci Rep 14, 30259 (2024). https://doi.org/10.1038/s41598-024-81349-3